## Slide 1: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Chapter 2
Electrostatic and thermodynamic potentials of electrons in materials
1. Electrostatic potential
2. Energies of free electrons and holes
3. Potential energy of the electrons in the semiconductor
4. The vacuum level
5. The Fermi level and the work function
6. The chemical potential of electrons
7. Potential step of a dipole layer or a double layer
8. Origin of surface dipoles
9. The Volta potential
10. Equalization of Fermi levels of two electronic conductor in contact
11. Equilibration of metal junctions and the contact potential difference
12. Equilibrium across the semiconductor junction

## Slide 2: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Chapter 1
Electrostatic and thermodynamic potentials of electrons in materials
1. Electrostatic potential
2. Energies of free electrons and holes
3. Potential energy of the electrons in the semiconductor
4. The vacuum level
5. The Fermi level and the work function
6. The chemical potential of electrons
7. Potential step of a dipole layer or a double layer
8. Origin of surface dipoles
9. The Volta potential
10. Equalization of Fermi levels of two electronic conductor in contact
11. Equilibration of metal junctions and the contact potential difference
12. Equilibrium across the semiconductor junction

## Slide 3: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.1. Energy diagram of an n-type doped semiconductor showing upward bandbending at the surface. (a) Reference energy level , local vacuum level , energy band edges and , the Fermi level , the chemical potential , the electron affinity , work function and ionization energy (hole affinity ). The subscript s denotes the value at the surface. (b) Local electric potential.
1. Electrostatic potential

## Slide 4: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.2. (a) Energy of the conduction band (edge energy ) and valence band (edge energy ) electronic states, as a function of electron momentum, in a semiconductor of bandgap energy . The vertical arrows indicate photoexcitation events that promote electrons from the valence band to the conduction band. (b) The density of states in the conduction band, showing the states filled with electrons up to the Fermi level at .
The occupancy probability of a level at energy
E is given by the Fermi-Dirac distribution function
effective density of states
2. Energies of free electrons and holes
3. Potential energy of the electrons in the semiconductor
the Fermi level of the electrons,

## Slide 5: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.3. (a) The distribution of crystal potential of a 5-layer Au(111) slab. Also indicated is the metal Fermi energy , and its work function. (b) Potential of the self-assembled monolayers (SAM) adsorbed onto Au(111). The HOMO is located at below . Also indicated is the vacuum level, and the modified work function of Au depending on the end group at the SAM. Adapted with permission from Heimel, G.; Romaner, L.; Bredas, J.-L.; Zojer, E. "Interface energetics and level alignment at covalent metal-molecule junctions: conjugated thiols on gold". Physical Review Letters 2006, 96, 196806.
The crystal forms a quantum well so that the energy of the electrons is lower inside the material than when extracted outside the surface
The analysis of changes of energies of electrons across different phases needs to be based on thermodynamic states of the electrons.
4. The vacuum level
5. The Fermi level and the work function

## Slide 6: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.4. Energy diagram of a metal, showing the crystal potential ɸ(x), and the local (Galvani) potential due to surface dipole and unscreened charge, j(x), that changes the local vacuum level.
we normally simplify the energy diagram of a metal as shown in Fig. 2.4, that illustrates the crystal potential as well as the local electrostatic potential
The horizontal part outside of the solid is the VL. If the electron gains enough energy to overcome the VL, it can escape from the solid.

## Slide 7: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.5. (a) Energy diagram of a semiconductor indicating the energy band edges EC and EV, vacuum level Evac, the Fermi level EFn, the electron affinity , work function ɸsc and ionization energy . (b) The local, surface and infinite vacuum level.
The electron affinity
is the energy required to excite an electron from the conduction band to the VL

## Slide 8: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.5. (a) Energy diagram of a semiconductor indicating the energy band edges EC and EV, vacuum level Evac, the Fermi level EFn, the electron affinity , work function ɸsc and ionization energy . (b) The local, surface and infinite vacuum level.
in many applications the zero of energy scale is placed at
The work function,
difference in energy of an electron at rest in vacuum just outside the surface and an electron at the Fermi energy into the solid

## Slide 9: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.7. Work functions of metals and contact materials, energy levels of inorganic and organic semiconductors and photoactive molecules, redox level of electrode materials, reactions in aqueous solution, and reference electrodes.

## Slide 10: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.6. (a) Energy diagram of a semiconductor indicating the reference energy level E0,ref , the vacuum level Evac , energy band edges Ec and Ev, and the different statistical quantities defined in the text.
the Fermi level of the electrons, is the same as the electrochemical potential of the electrons
the Fermi level of the holes is drawn in the electron energy scale
the total electrochemical energy of an electron-hole pair
6. The chemical potential of electrons

## Slide 11: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.8. Energy diagram of an n-type doped semiconductor at two points with different values of the chemical potential µn. Ec is the conduction band edge, EFn is the Fermi level. The increase of the chemical potential ∆µn>0 produces a larger concentration of electrons in the conduction band.

## Slide 12: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.9. (a) Energy diagram of a dipole layer consisting on two sheets of negative and positive charge separated a distance d. is the electrostatic potential, E is the electric field and ∆d is the step of the vacuum energy across the dipole layer. (b) Energy diagram (vacuum level) of a dipole layer of polar molecules with dipole moment md that are tilted an angle θ with respect to the normal.
7. Potential step of a dipole layer or a double layer

## Slide 13: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.10. Energy diagram (vacuum level) of a dipole layer of finite extension.
when removing the electron a distance
, the dipole layer can be considered a point dipole and the electrostatic potential decreases rapidly

## Slide 14: Reproduced with permission from Crispin, X.; Geskin, V.; Crispin, A.; Cornil, J.; Lazzaroni, R.; Salaneck, W. R.; Bredas, J.-L. "Characterization of the interface dipole at organic/metal interfaces". J. Am. Chem. Soc. 2002, 124, 8131-8141. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.12. DFT calculations within the jellium model give the evolution of the electron density across the metal/vacuum interface (bottom dotted curve), the effective potential (top dotted curve), and the electric potential (top solid line). The large circles depict the atoms on the metal surface; the zero on the x axis is positioned at one-half the interatomic layer distance from the surface nuclei plane (x > 0 indicates the metal bulk). f(x) is a fitting sigmoid function.
8. Origin of surface dipoles

## Slide 15: Adapted with permission from Heimel, G.; Romaner, L.; Bredas, J.-L.; Zojer, E. "Interface energetics and level alignment at covalent metal-molecule junctions: conjugated thiols on gold". Physical Review Letters 2006, 96, 196806. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.3. (a) The distribution of crystal potential of a 5-layer Au(111) slab. Also indicated is the metal Fermi energy , and its work function. (b) Potential of the self-assembled monolayers (SAM) adsorbed onto Au(111). The HOMO is located at below . Also indicated is the vacuum level, and the modified work function of Au depending on the end group at the SAM.
the end group of the molecular layer is crucial to determine the Au slab work function.

## Slide 16: Adapted with permission from Ishii, H.; Sugiyama, K.; Ito, E.; Seki, K. "Energy level alignment and interfacial electronic structures at organic/metal and organic/organic interfaces". Advanced Materials 1999, 11, 605. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.11. Energy diagram of an electron in and out of a metal crystal. The different crystal facets produce different surface dipole and change the work function ɸ.
The surface dipole is indicated by a step change of the local electrostatic potential
and the corresponding step of the VL

## Slide 17: Reproduced with permission from Fukagawa, H.; Yamane, H.; Kera, S.; Okudaira, K. K.; Ueno, N. "Experimental estimation of the electric dipole moment and polarizability of titanyl phthalocyanine using ultraviolet photoelectron spectroscopy". Phys. Rev. B 2006, 73, 041302. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.13. Dependence of work function on OTiPc coverage. This molecule has an electric dipole moment perpendicular to the molecular plane. The schematic representation of the molecular orientation and the direction of the dipole in the monolayer of OTiPc are indicated. In the low coverage region ( 0.3 ML), the work function changes along the dashed line (a). The thin curves represent fitting curves to different models model.

## Slide 18
Figure 2.14. Energy diagram of an electron in and out of a semiconductor crystal with a surface dipole.
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
9. The Volta potential
It is useful to consider that the work function, which is the work to extract an electron from the material, consists of two parts: the specific binding energy of the electron in the bulk material, and the work required to move the electron across the surface dipole layer.
so that it consists of an intrinsic work function and the surface polarization term
The electrostatic potential, at the surface, is called the Volta potential

## Slide 19
Figure 2.15. (a) Metal blocks of different work function. (b) The Volta potentials caused by net charges in each plate and the contact potential difference between the two metals when the Fermi levels are in equilibrium. (c) The metal surfaces in contact.
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
10. Equalization of Fermi levels of two electronic conductors in contact
If two electronic systems come into contact, as shown in Fig. 2.15, and the electrons have different electrochemical potentials in the two systems, there will be a transference of electrons from the system with the higher electrochemical potential to that with the lower
.

## Slide 20
Figure 2.15. (a) Metal blocks of different work function. (b) The Volta potentials caused by net charges in each plate and the contact potential difference between the two metals when the Fermi levels are in equilibrium. (c) The metal surfaces in contact.
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
11. Equilibration of metal junctions and the contact potential difference
.
the contact potential difference (CPD).
The built-in potential is the final step of the VL

## Slide 21
Figure 2.16. Energy diagram of potentials, vacuum levels, and Fermi levels, in two metal crystals.
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
The difference of the Volta potentials
can be measured
In the case that the Fermi levels line up, is measured by Kelvin probe method or photoelectron spectroscopies . The Volta potential difference
corresponds rigorously with the CPD

## Slide 22
Figure 2.17. Energy diagram of two semiconductors in contact in different situations: (a) Nonequilibrium situation. The two materials are not in equilibrium as the electron Fermi level EFn is higher in the material at the left side. This causes electron transfer towards the material at the right side. (b) Equilibrium situation. The electron transfer causes a rearrangement of the potential difference between the materials that is reflected in the step of the vacuum energy, which equals de difference of the work functions of the materials, and a change in the conduction band offset Ec2 – Ec1. Now electrons have the same free energy at both sides of the interface and the net flux across the interface is zero.
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press

## Slide 23
Figure 2.18. Energy diagram of two pieces of semiconductor with different doping that form a p-n junction. (a) The left piece is n-doped, and the right one is p-doped. (b) When the materials come to contact, electronic equilibrium is established equalizing the Fermi level by means of a space charge region that produces band bending at the junction.
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
12. Equilibrium across the semiconductor junction

## Slide 24
© Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Recommended References
Guggenheim, E. A. "The conceptions of electrical potential difference between two phases and the individual activities of ions". The Journal of Physical Chemistry 1929, 33, 842.
Ishii, H.; Sugiyama, K.; Ito, E.; Seki, K. "Energy level alignment and interfacial electronic structures at organic/metal and organic/organic interfaces". Advanced Materials 1999, 11, 605.
Marshak, A. H. "Modeling Semiconductor Devices with Position-Dependent Material Parameters". IEEE Trans. El. Dev. 1989, 36, 1764-1772.
Würfel, P. Physics of Solar Cells. From Principles to New Concepts; Wiley: Weinheim, 2005.