## Slide 1: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Chapter 3
The voltage, capacitors, and batteries
1. The voltage in the device
2. Anode and cathode
3. Applied voltage and potential difference
4. The capacitor
5. Measurement of the capacitance
6. Energy storage in the capacitor
7. Electrochemical systems. Structure of the metal/solution interface
8. Electrode potential and reference electrodes
9. The redox potential in electrochemical cells
10. Electrochemical and physical scales of electron energy in material systems
11. Changes of electrolyte levels with pH
12. Principles of electrochemical batteries
13. Capacity and energy content
14. Practical electrochemical batteries
15. The Li ion battery

## Slide 2: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.1. Basic structure of a device. (a) Planar geometry. (b) Nanostructured particulate semiconductor contacts current collector including a blocking layer and is surrounded by liquid electrolyte that contacts the right electrode
1. The voltage in the device
devices are contacted by a high conductivity material, that does not undergo chemical transformations, and such material is often termed the current collector. Other common denominations of the contacts are the electrodes, the plates, or the terminals. The electrode is sometimes extended to include active phases in the device, as well as the first layers of electrolyte in contact with the solid.
Nanostructured energy devices usually operate by the combination of several materials arranged to funnel the charge carriers in a desired direction, or to provoke required chemical reactions.

## Slide 3: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 1.2. SEM image of the cross section of a porous electrode formed by sintered TiO2 anatase crystals (inset), deposited on a transparent substrate that consists on a glass support and thin TCO layer. Courtesy of Ronen Gottesman and Arie Zaban.

## Slide 4: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.2. The voltage applied in the device, V , is proportional to the difference of the electron Fermi level in the left electrode EFA, and the electron Fermi level in the right electrode, EFB , which is taken as a graphical reference. The vertical scale represents electron energy increasing upwards. (a) Negative bias voltage at the left electrode. (b) Positive bias voltage at the left electrode.
The voltage measures the work necessary to carry an electron from one plate of the device to the other.
2. Anode and cathode
The voltage is given by the difference of electron Fermi levels (electrochemical potential of electrons) between the two plates

## Slide 5: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.3. (a) Negative bias at the left electrode of a diode. Electrons enter the diode at the negative electrode, the cathode. (b) The battery produces negative voltage at the left electrode. Electrons leave the battery through the negative terminal, and enter the battery through the positive terminal, which is the cathode.
If the device is a load such as a resistor it consumes electric power. The voltage has to be applied from an external power source, for example using a battery.
If the device itself produces power such as a battery, or a solar cell, voltage exists even in the absence of any external power source,

## Slide 6: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.3. (a) Negative bias at the left electrode of a diode. Electrons enter the diode at the negative electrode, the cathode. (b) The battery produces negative voltage at the left electrode. Electrons leave the battery through the negative terminal, and enter the battery through the positive terminal, which is the cathode.
in a device which consumes power as an electrolyzer, the cathode is at negative voltage with respect to the anode, and
in a device which provides power, the cathode is at positive potential.
In a battery, the sign of the current changes when the battery is being charged or discharged. Irrespective of the current flow, the electrode containing the more electropositive material, that is with lower work function (for example, graphite in a lithium-ion cell) is termed the anode.

## Slide 7: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
3. Applied voltage and potential difference
Figure 3.5. Energy diagram of potentials, vacuum levels, and Fermi levels, in two metal contacts of the same material.

## Slide 8: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.4. Measurement of voltage between pieces of silver and gold, using a voltmeter that has copper terminals.
Terminals of the same material
A voltage in a device is a difference of Fermi levels between the two electrodes.
the difference of electrostatic potentials is not the voltage.
if the contacts materials are different, there is a difference of Volta and Galvani potentials.
the voltmeter provides the difference of electrochemical potentials (Fermi levels) of electrons between Ag and Au, though not the electric potential difference

## Slide 9: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.6. A capacitor formed by two plates of the same metal. (a) Zero voltage. (b) The left plate in biased negatively.
4. The capacitor

## Slide 10: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.7. A capacitor formed by two plates of different material. (a) The separate materials. (b) The capacitor at zero voltage. (c) The capacitor biased negatively at the left contact. The built-in potential is

## Slide 11: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Capacitors involving displacement current will be here called a dielectric capacitor, to distinguish from a chemical capacitance and electrochemical capacitance

## Slide 12: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press

## Slide 13: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
6. Energy storage in the capacitor

## Slide 14: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.8. Structure of the Helmholtz layer at the contact between the metal electrode and an electrolyte. (a) At zero applied potential, a contact potential difference is built (that accommodates the difference between the metal work function and the redox energy of the electrolyte), consisting of a voltage drop VH , across the interfacial dipole formed by electrons at the metal surface and ions at the solution side. (b) With a negative applied potential, the amount of positive and negative charge at the surface increases, and so does the interfacial potential drop VH.
7. Electrochemical systems. Structure of the metal/solution interface
20 mF cm-2
faradaic and nonfaradaic current

## Slide 15: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.9. Scheme of an electrochemical cell, consisting on the working electrode (WE), counterelectrode (CE) and reference electrode (RE). The potential is measured with respect to a reference electrode in solution, which in this case is the SHE defined in terms of the H+/H2 couple at pH = 0. The voltage V is a difference of Fermi levels between the Fermi level of electrons in the metal WE, EF , and the Fermi level of the metallic contact to the SHE. (a) Measurement of the redox potential, . (b) Determination of the overpotential at the WE when the cell is under applied voltage. The overpotential Vn is the difference between the potential of the Fermi level in the metal WE and the equilibrium (redox) potential (indicated as a redox energy level ). The applied voltage Vapp is related to the difference of Fermi levels between WE and CE.
8. Electrode potential and reference electrodes
2 H+ + 2 e-
standard hydrogen electrode, SHE.
H2 gas at a pressure of 1 atmosphere, bubbled over platinum in an electrolyte in which the activity of hydrogen ions (not atoms or molecules) is unity (water at pH 0)

## Slide 16: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
9. The redox potential in electrochemical cells
(10)

## Slide 17: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
(10)
10. Electrochemical and physical scales of electron energy in material systems
The difference between the absolute scale, and SHE scale, is the energy of the hydrated proton at unit activity, with respect to the electron in vacuum close to the solution surface (Trasatti, 1986), which is about
= - 4.44 eV.
Figure 3.10. (a) Measurement of energy of a specific energy level, E, from the vacuum level, or as potential Vr from the reference electrode.

## Slide 18: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 2.7. Work functions of metals and contact materials, energy levels of inorganic and organic semiconductors and photoactive molecules, redox level of electrode materials, reactions in aqueous solution, and reference electrodes.

## Slide 19: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.10. (a) Measurement of energy of a specific energy level, E, from the vacuum level, or as potential Vr from the reference electrode. (b) Energy level of metal/semiconductor/electrolyte system, before they reach equilibrium of equalized Fermi levels.

## Slide 20: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
11. Changes of electrolyte levels with pH
The parameter pH measures the activity of H3O+ ions as
pH =
= 1.008
The constant is the ionic product of water. In neutral water the concentrations of both ionic species are the same, 10-7 mol L-1, and the value of pH is 7.
mol2 L-2
= 1.008

## Slide 21: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 3.11. General form of water reduction and oxidation potentials, vs. pH, or Pourbaix, diagram. The shaded region is the domain of stability of water. At more negative potentials than the upper water is reduced by electrons injected from the electrode, and at more positive potentials water is oxidized by holes injected from the electrode. At acid pH proton (hydronium) ions are more abundant, while at alkaline pH the hydroxyl ion OH- dominates, and the reduction and oxidation reactions are expressed differently.

## Slide 22: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
References
Rickert, H. Electrochemistry of Solids; Springer Verlag: Berlin, 1982.
Riess, I. "What does a voltmeter measure?" Solid State Ionics 1997, 95, 327-328.
Trasatti, S. "The absolute electrode potential: An explanatory note". Pure and Applied Chemistry 1986, 58, 955-966.