## Slide 1: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Chapter 5
Thermal distribution of electrons, holes and ions in solids
1. Equilibration of the electrochemical potential of electrons
2. Configurational entropy of weakly interacting particles
3. Equilibrium occupancy of conduction band and valence band states
4. The equilibrium Fermi level and the carrier number in semiconductors
5. Transparent conducting oxides
6. Hot electrons
7. Screening
8. The rectifier at forward and reverse voltage
9. Semiconductor devices as thermal machines that realize useful work
10. Cell potential in the lithium ion battery
11. Insertion of ions: the lattice gas model

## Slide 2: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
1. Equilibration of the electrochemical potential of electrons
Helmholtz free energy

## Slide 3: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
2. Configurational entropy of weakly interacting particles
is the number of electrons then
sites are occupied and
are empty

## Slide 4: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.1. (a) The Fermi-Dirac distribution at different values of the Fermi level at . The vertical axis is the level energy and the lower axis is the occupancy. At the right is shown a particular level representing a localized level in the bandgap. At the trap level is exactly half-occupied. (b) The same distributions in log scale, showing the occupancy of the conduction band level. The numbers on the top axis is the electron density for a total density of states . © Juan Bisquert
3. Equilibrium occupancy of conduction band and valence band states

## Slide 5: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.2. (a) The Fermi-Dirac distribution at different temperatures for a Fermi level at . The vertical axis is the level energy and the lower axis is the occupancy. At the right is shown a particular level representing a localized level in the bandgap. At the trap level is exactly half-occupied. (b) The same distributions in log scale, showing the increasing occupancy of the conduction band level as becomes smaller. © Juan Bisquert

## Slide 6: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.3. Energy diagram of a p-type semiconductor layer. is the bandgap energy, is the energy of the conduction band, is the energy of the valence band, is the intrinsic energy level, is the equilibrium Fermi level, is the electron Fermi level, is the hole Fermi level, is the elementary charge and is the voltage. (a) Zero bias. (b) Forward bias increases the population of electrons in the conduction band. © Juan Bisquert
equilibrium Fermi level

## Slide 7: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.4. The intrinsic carrier concentration of silicon as function of temperature. © Juan Bisquert

## Slide 8: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
4. The equilibrium Fermi level and the carrier number in semiconductors

## Slide 9: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.5. (a) DOS in the conduction and valence bands. (b) Energy distribution of the populations of electrons and holes in electrochemical equilibrium at room temperature. (c) Electrons and holes thermalized in the respective bands at room temperature at separate Fermi levels. © Juan Bisquert
There are separate equilibria to the assemblies of electrons in the conduction band, on the one hand, and those in the valence band, in the other

## Slide 10: . Reproduced with permission from Klein, A. "Transparent conducting oxides: electronic structure–property relationship from Photoelectron Spectroscopy with in situ sample preparation". Journal of the American Ceramic Society 2013, 96, 331–345. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.6. Top: Fermi levels of ZnO, In2O3, and SnO2 determined from in situ photoelectron spectroscopy measurements of films prepared by magnetron sputtering. Each data point has been recorded from a separate film. Bottom: Correlation between electrical and optical properties and the Fermi level position obtained from in situ XPS measurements of the same films performed right after deposition: (a) electrical conductivity, (b) optical band gap. The dashed line in (a) corresponds to a calculated conductivity using a parabolic conduction band.
5. Transparent conducting oxides

## Slide 11: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.7. The absorption of a photon of energy hv promotes the photoexcitation of an electron to the conduction band, that lies in a high energy state for a short time. Thereafter the hot electron cools to the bottom of the conduction band in states of energy Ec. © Juan Bisquert
6. Hot electrons

## Slide 12: Reproduced with permission from Konig, D.; Casalenuovo, K.; Takeda, Y.; Conibeer, G.; Guillemoles, J. F.; Patterson, R.; Huang, L. M.; Green, M. A. "Hot carrier solar cells: Principles, materials and design". Physica E: Low-dimensional Systems and Nanostructures 2010, 42, 2862-2866. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.8. Carrier cooling kinetics in bulk semiconductor: Thermal equilibrium (0); immediately after optical generation (1); carrier–carrier scattering, impact ionisation, re-normalisation of carrier energies, Fermi–Dirac statistics (2); optical phonon emission (re-absorption) (3); decay of optical into acoustic phonons (4); further phonon emission (5), to thermal equilibrium, onset of carrier recombination (6).

## Slide 13: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.9. Electrons and holes in electrochemical equilibrium at high temperature. © Juan Bisquert
The carriers may equilibrate among themselves, at a higher temperature than the ambient temperature

## Slide 14: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
7. Screening
Figure 5.10. The Debye screening length as function of background density of carriers for different values of dielectric constant of the medium.

## Slide 15: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.11. Model diode, of p-type semiconductor material, with an electron selective contact at the left side and a hole selective contact at the right side, indicating the voltage, Fermi levels, internal and external currents, and the balance of incoming and outgoing photons absorbed or produced in the material. (a) The diode in dark equilibrium. The generation by incoming thermal radiation is balanced by recombination that corresponds to reverse saturation current. All recombination is radiative. (b) Under applied bias voltage in the dark carriers are injected (a positive voltage increases minority carrier density) and the recombination of carriers is greatly increased. The diode emits light corresponding to the energy of the bang gap. (c) At reverse voltage the internal current generated in equilibrium is extracted (reverse saturation current). © Juan Bisquert
8. The rectifier at forward and reverse voltage
In general a forward voltage is:
-a negative potential applied to the electron selective contact or
-a positive potential applied to the hole selective contact.
The reverse voltage is defined as:
-a positive potential applied to the electron selective contact or
-a negative potential applied to the hole selective contact.

## Slide 16: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.12. Energy diagram of a p-type semiconductor layer with electron selective contact at the left side and hole selective contact at the right side. q is the elementary charge, V is the voltage at the left terminal, Ec is the energy of the conduction band, Ev is the energy of the valence band, EF0 is the equilibrium Fermi level, EFn is the electron Fermi level, EFp is the hole Fermi level. (a) Zero bias in dark. Blackbody radiation produces generation of electron-hole pairs (1). The dark generation achieves equilibrium with recombination (2) of electrons and holes. (b) Forward bias injects electrons (1) and holes (2) and causes recombination (3). (c) Reverse bias causes modification of the interfaces, the only current is due to thermal generation of carriers that are extracted. The Fermi level of electrons is not shown in the semiconductor material. © Juan Bisquert

## Slide 17: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.13. Current density-voltage characteristics characteristic of a diode with reverse saturation current j0.

## Slide 18: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.14. Operation of a semiconductor device by transference of electrons through the external circuit. © Juan Bisquert
9. Semiconductor devices as thermal machines that realize useful work

## Slide 19: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.15. Energy exchanges in difference processes involving an external load of battery, the set of electrons and holes, and the semiconductor lattice. (a) Application of the voltage creates carriers to split the Fermi levels. (b) Nonradiative recombination, converts carriers to heat. (c) The electron system does work on the load. (d) Radiative recombination while the number of electrons and holes is kept constant by the applied voltage. © Juan Bisquert

## Slide 20: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.15. Energy exchanges in difference processes involving an external load of battery, the set of electrons and holes, and the semiconductor lattice. (a) Application of the voltage creates carriers to split the Fermi levels. (© Juan Bisquert
the lattice is actually cooled

## Slide 21: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.15. Energy exchanges in difference processes involving an external load of battery, the set of electrons and holes, and the semiconductor lattice. (b) Nonradiative recombination, converts carriers to heat. © Juan Bisquert
the free energy of the electrons, that could have been used to do work

## Slide 22: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.15. Energy exchanges in difference processes involving an external load of battery, the set of electrons and holes, and the semiconductor lattice. (c) The electron system does work on the load. © Juan Bisquert

## Slide 23: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 5.15. Energy exchanges in difference processes involving an external load of battery, the set of electrons and holes, and the semiconductor lattice. (d) Radiative recombination while the number of electrons and holes is kept constant by the applied voltage. © Juan Bisquert
The process can be reversed if a light source is available that contain photons that can be absorbed by the semiconductor generating electron hole pairs.