## Slide 1: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Chapter 6
Interfacial kinetics and hopping transitions
1. Detailed balance principle
2. Form of the transition rates
3. Kinetics of localized states: Shockley-Read-Hall recombination model
4. Reorganization effects in charge transfer: the Marcus model
5. Polaron hopping
6. The rate of electrode reaction: Butler-Volmer equation
7. Electron transfer at metal-semiconductor contact
8. Electron transfer at semiconductor/electrolyte interface

## Slide 2: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.1. (a) Carrier transfer between two types of electronic states, at energies and , with local Fermi levels and , respectively. (b) Carrier transfer between three different types of states.
1. Detailed balance principle
detailed balance condition imposes the constraint that in the equilibrium steady state, the flux of forward and backward transitions between a pair of states balance in detail.

## Slide 3: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.2. Structure of LiFePO4 (Fig. 5.17) depicting the curved trajectory of Li ion transport along the b-axis, shown with red arrows. The iron octahedra are shown in blue, the phosphate tetrahedral in yellow, and the lithium ions in green . Reproduced with permission from Ellis, B. L.; Lee, K. T.; Nazar, L. F. "Positive electrode materials for Li-ion and Li-batteries". Chemistry of Materials 2010, 22, 691-714.

## Slide 4: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.1. (a) Carrier transfer between two types of electronic states, at energies and , with local Fermi levels and , respectively. (b) Carrier transfer between three different types of states.
master equation

## Slide 5: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Arrhenius
Polaron

## Slide 6: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.3. Schematic illustration of the double-layer structure during oxygen reduction reaction in alkaline media, showing different species in solution. Inset (a), illustrates the inner-sphere electron transfer processes for the reduction of an absorbed molecule at the electrode surface (inner Helmholtz plane). Inset (b) shows an outer-sphere electron transfer for a solvated molecule close to the surface (outer Helmholtz plane). Reproduced with permission from Ramaswamy, N.; Mukerjee, S. "Fundamental mechanistic understanding of electrocatalysis of oxygen reduction on Pt and Non-Pt Surfaces: acid versus alkaline media". Advances in Physical Chemistry 2012, 2012, 491604.
Figure 3.9.

## Slide 7: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Miller-Abraham, Metropolis

## Slide 8: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Monte-Carlo simulation
Fig. 5.28

## Slide 9: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.4. Electronic processes in localized states: a trap, a recombination center, and a surface state.
3. Kinetics of localized states: Shockley-Read-Hall recombination model

## Slide 10: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.4. Electronic processes in localized states: a trap, a recombination center, and a surface state.

## Slide 11: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.5. Top: Energy diagram of a donor-acceptor system, showing, at the left, the “reactant” state which is the relaxed excited state D*A0, and at the right, the charge separated (“product”) state D+A-. Bottom: polarization in different stages of the DA system. In the center of the sphere is indicated the state of charge Q of each element. At the right is shown the potential energy of the reactants UR and the products state Up, as a function of the nuclear coordinates. (a) The solvent in equilibrium with the reactant. (b) a nonequilibrium transition state in which the energy of the reactant state equals that of the product. (c) Solvent in equilibrium with the product.
4. Reorganization effects in charge transfer: the Marcus model

## Slide 12: Reproduced with permission Liu, T.; Troisi, A. "Absolute rate of charge separation and recombination in a molecular model of the P3HT/PCBM interface". The Journal of Physical Chemistry C 2011, 115, 2406-2415. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.6. Model of the electron transfer between the P3HT and PCBM interface. One PCBM molecule and one oligomer (regioregular) containing six thiophene rings (hexyl groups on P3HT are replaced by methyl groups) are displayed, showing the frontier orbitals involved in the excitation processes obtained by the DFT method: an electron in the LUMO of P3HT and electron in the LUMO of PCBM.

## Slide 13: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.7 Free energy curves for an electron transfer reaction showing the potential energy of the reactant state D*A0, UR , and the products state D+A-, UP , as a function of the nuclear coordinates and reaction coordinate. ∆G0 indicates the “standard” change of free energy from reactants (R) to products (P) and is negative in this case. The transition state activation free energy is ∆G*, which is actually the free energy barrier for the electron transfer. The reorganization energy is λ.

## Slide 14: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.7 Free energy curves for an electron transfer reaction showing the potential energy of the reactant state D*A0, UR , and the products state D+A-, UP , as a function of the nuclear coordinates and reaction coordinate. ∆G0 indicates the “standard” change of free energy from reactants (R) to products (P) and is negative in this case. The transition state activation free energy is ∆G*, which is actually the free energy barrier for the electron transfer. The reorganization energy is λ.

## Slide 15: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.8. Electronic potential-energy curves (on left) and the corresponding (nuclear) potential-energy curves on the right. The electronic energies in the two wells are indicated on the left for three nuclear configurations A, B, and C for the reaction red1 + ox2 ox1 + red2. The levels in the wells are vertical ionization energies: the filled and open circles denote, respectively, ionization of the reduced state at its equilibrium nuclear configuration and at the equilibrium configuration appropriate to its oxidized state; the half-filled circles refer to ionization of the reduced state at the nuclear configuration appropriate to the intersection region. The level in well 1 is initially occupied in (a) and the level in well 2 in (c). Reproduced with permission from Marcus, R. A.; Sutin, N. "Electron transfers in chemistry and biology". Biochimica et Biophysica Acta (BBA) - Reviews on Bioenergetics 1985, 811, 265-322.

## Slide 16: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.9. Free energy curves for the absorption and emission of photons between the ground (D) and excited state (D*) of a molecule. The photon energy for the maximal absorbance and emission are indicated, the reorganization energy λ for the relaxation of the first excited state after absorption, and the ground state after the emission of a photon by fluorescence.

## Slide 17: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
When the distance
is small, the reorganization energy
is smaller

## Slide 18: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.10. Free energy curves for an electron transfer reaction as a function of the nuclear coordinates and reaction coordinate for a self-exchange reaction in which the reactants and products are the same.

## Slide 19: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.11. Free energy curves for an electron transfer reaction as a function of the nuclear coordinates. The curves show a change of the product for an increasingly large driving force ∆G0 , until the transition state activation free energy ∆G* , passes through value 0 and starts to increase in the Marcus inverted region, as shown in the inset.

## Slide 20: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.12. (a) Stabilization of a carrier in a solid medium by interaction with phonons, to form a polaron. The graph shows the modification of the elastic energy for a single carrier for the interaction of the carrier with the lattice. (b) Effective potential wells for two sites, showing in each case the situation when the carrier is within the site. Also indicated is a vertical optical transition.
5. Polaron hopping
for
and
(7)

## Slide 21: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.12. (a) Stabilization of a carrier in a solid medium by interaction with phonons, to form a polaron. The graph shows the modification of the elastic energy for a single carrier for the interaction of the carrier with the lattice. (b) Effective potential wells for two sites, showing in each case the situation when the carrier is within the site. Also indicated is a vertical optical transition.
5. Polaron hopping
(7)

## Slide 22: Reproduced with permission from Watanabe, M.; Hayashi, T. "Time-resolved study of self-trapped exciton luminescence in anatase TiO2 under two-photon excitation". Journal of Luminescence 2005, 112, 88-91 and Pallotti, D. K.; Orabona, E.; Amoruso, S.; Aruta, C.; Bruzzese, R.; Chiarella, F.; Tuzi, S.; Maddalena, P.; Lettieri, S. "Multi-band photoluminescence in TiO2 nanoparticles-assembled films produced by femtosecond pulsed laser deposition". Journal of Applied Physics 2013, 114, 043503. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.12. Luminescence (dotted line) and excitation (solid line) spectra of anatase TiO2 at low temperature (top) and luminescence at room temperature of several samples (bottom).

## Slide 23: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.13. Schematic representation of the initial stages of a photoinduced process in anatase TiO2: creation of a bulk exciton upon light irradiation, formation of self-trapped polarons at bulk lattice sites, and polarons trapped at surface sites. Reproduced with permission from Di Valentin, C.; Selloni, A. "Bulk and surface polarons in photoexcited anatase TiO2". The Journal of Physical Chemistry Letters 2011, 2, 2223-2228.

## Slide 24: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.15. Structure of the Helmholtz layer at the contact between the metal electrode and an electrolyte, containing solvated redox species and salt anions and cations, and the events of interfacial charge transfer that constitute electrochemical reactions. (a) At zero applied potential, a contact potential difference is built, consisting of a voltage drop VH, across the interfacial dipole formed by electrons at the metal surface and ions at the solution side. The reduction and oxidation reactions flow at the same rates. (b) With a negative applied potential, the amount of positive and negative charge at the surface increases, and so does the interfacial potential drop VH. The increase of the voltage across the interface increases the rate of the cathodic (reduction) reaction.
6. The rate of electrode reaction: Butler-Volmer equation

## Slide 25: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.16. Scheme of electrode reactions in electron energy scale. The potential Vr is the voltage applied to the electrode with respect to a reference electrode in solution. The overpotential Vn is the difference between the electrode potential and the equilibrium redox potential Vredox . (a) The overpotential Vn is negative and promotes the cathodic reaction, since the electron energy level is above the redox level. (b) The overpotential is positive and promotes the anodic reaction at the electrode surface, as the electron energy at the metal is below the redox level.

## Slide 26: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.17. Scheme of an electrochemical cell, consisting on an electrolyte between two metal plates of the same material. (a) At the surface of the negative biased (left) electrode the oxidized A+ ionic species in solution is reduced to A0. At the positive biased (right) electrode the reduced species A0 is oxidized to A+. The flow of A0 and A+ in the electrolyte is indicated. (b) The electric current is equal to the discharge of electrons at the negative electrode, which is proportional to the surface concentration of A0 at the surface of the electrode. Mass transport in the electrolyte is controlled by diffusion across a boundary layer of thickness δ.
Availability of electronic species
Availability of redox species.

## Slide 27: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.18. Free energy diagram for a one electron transfer showing the change of free energy curves of ox and red species as a function of the overpotential Vn . β is the symmetry factor.
The kinetic constant for charge transfer

## Slide 28: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.19. (a) Current-overvoltage curve for the cathodic and anodic reactions at the metal/electrolyte interface. The exchange current density is , and . (b) Current-overvoltage curve for the cathodic reaction.

## Slide 29: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.20. (a) Current-overvoltage curve for the cathodic and anodic reactions at the metal/electrolyte interface. The exchange current density is indicated, and . (b) The current at low overvoltage. (c) The current in log scale.

## Slide 30: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.21. (a) The lowering of interfacial barrier by image force effect. (b) Thermally assisted Fowler-Nordheim tunneling. (c) Tunneling at the Fermi level.
7. Electron transfer at metal-semiconductor contact

## Slide 31: Reproduced with permission from Scott, J. C. "Metal--organic interface and charge injection in organic electronic devices". Journal of Vacuum Science & Technology A: Vacuum, Surfaces, and Films 2003, 21, 521-531. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.22. Energetics of the charge injection process. Electrons in extended states in the metal, including those thermally excited above the Fermi level, tunnel into localized states in the semiconductor, where there are four contributions to the energy: the barrier height, the image potential, the potential due to the interfacial electric field, and a random component due to disorder.

## Slide 32: Reproduced with permission from Baldo, M. A.; Forrest, S. R. "Interface-limited injection in amorphous organic semiconductors". Physical Review B 2001, 64, 085201 Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.23. (a) Two-step process injection model. Charges are initially injected into an interface region where the distribution of energy sites is broadened by interface dipoles. The limiting step is the hop from the interfacial region into the bulk distribution. (b) The interface is modeled by a collection of point dipoles. In the bulk, each site is randomly oriented but at the interface the dipoles are oriented in a Gaussian distribution about the perpendicular ( θ=0). (c) The effect of the interface dipoles on the electron-energy distribution in the bulk is calculated. The distribution in the first few organic monolayers is considerably broadened. With increasing distance, the energetic distribution, approaches the bulk distribution.

## Slide 33: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.24. Charge transfer from a semiconductor, to the fluctuating energy levels of the ox and red species in electrolyte with a reorganization energy .
8. Electron transfer at semiconductor/electrolyte interface

## Slide 34: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.24. Charge transfer from a semiconductor, to the fluctuating energy levels of the ox and red species in electrolyte with a reorganization energy .

## Slide 35: Reproduced with permission from Morisaki, H.; Ono, H.; Yazawa, K. "Measurement of the density of electronic states in aqueous electrolytes using oxide-covered Pt-silicide electrodes". Journal of The Electrochemical Society 1988, 135, 381-383. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.25. (a) Current density vs. surface potential characteristics, as well as the potential derivatives ( ) of an oxide-covered Pt-silicide electrode measured in a 0.1M-Fe(CN)63-/4- and 0.5M-Na2SO4 electrolyte. The broken line is an I-V characteristic for a Pt electrode measured in the same electrolyte. (b) Effective density of electronic states for ferrocyanic ions deduced from a method that uses . The continuous line is the theoretical expression of the Marcus-Gerischer model, using a reorganization energy of 0.6 eV.

## Slide 36: Reproduced with permission from Hamann, T. W.; Gstrein, F.; Brunschwig, B. S.; Lewis, N. S. "Measurement of the free-energy dependence of interfacial charge-transfer rate constants using ZnO/H2O semiconductor/liquid contacts". Journal of the American Chemical Society 2005, 127, 7815-7824. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.26. The dependence of electron-transfer rate constants on the driving force for interfacial charge transfer from n-type ZnO electrodes in aqueous solutions to a series of nonadsorbing, one electron, outer-sphere redox couples with formal reduction potentials that span approximately 900 mV.

## Slide 37: Reproduced with permission from Gerischer, H. "The impact of semiconductors on the concepts of electrochemistry". Electrochimica Acta 1990, 35, 1677-1699. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.27. Redox reactions at n-type (a) and p-type (b) semiconductor electrodes. Above: typical energy correlations at a particular voltage . Below: current-voltage curves.

## Slide 38: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.28. The semiconductor/electrolyte interface forms a selective contact to electrons in the semiconductor when the energy level of the semiconductor conduction band minimum matches well those of oxidized species in the electrolyte, while the transference of holes across the interface is hindered by slow kinetics.

## Slide 39: Reproduced with permission from Nozik, A. J.; Memming, R. "Physical chemistry of semiconductor-liquid interfaces". The Journal of Physical Chemistry 1996, 100, 13061-13078. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.29. Sequence of energy level diagrams for a semiconductor-metal photoelectrolysis cell from the initial condition (no contact and no electrochemical potential equilibration) to the final condition of photoelectrolysis of water with an external bias.

## Slide 40: Reproduced with permission from Salvador, P.; Gutierrez, C. "The nature of surface states involved in the photo- and electroluminescence spectra of n-titanium dioxide electrodes". The Journal of Physical Chemistry 1984, 88, 3696-3698. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.30. Energy level diagram of the n-TiO2/electrolyte interface including redox potentials of electrolyte couples.

## Slide 41: Reproduced with permission from Nozik, A. J.; Memming, R. "Physical chemistry of semiconductor-liquid interfaces". The Journal of Physical Chemistry 1996, 100, 13061-13078. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 6.31. Energy level diagram for the photoelectrolysis of water using the single, wide band gap semiconductor strontium titanate (SrTiO3). The photoelectrolysis reaction can proceed without an external bias because the conduction and valence band edges straddle the redox potentials for the hydrogen and oxygen evolution reactions.