## Slide 1: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Chapter 7
The chemical capacitance
1. Carrier accumulation and energy storage
2. Localized electronic states in disordered materials and surface states
3. Chemical capacitance of a single state
4. Chemical capacitance of a broad DOS
5. Filling a DOS with carriers: the voltage and the conductivity
6. Chemical capacitance of Li intercalation materials
7. Chemical capacitance of graphene

## Slide 2: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.1. (a) Representation of a dielectric capacitor, showing the vacuum level (VL), the electrical charge at the plates, and the electrical field, , in the space between the plates. (b) A semiconductor with selective contacts. Under applied bias the position of the Fermi level of minority carriers changes which produces variation of the chemical potential of the electrons,
1. Carrier accumulation and energy storage in the chemical capacitance

## Slide 3: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.1.
Figure 7.7
Figure 1.5

## Slide 4: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.2. Schematic diagram of crystal structures and electronic states in a semiconductor film. Reproduced with permission from Schultze, J. W.; Lohrengel, M. M. "Stability, reactivity and breakdown of passive films. Problems of recent and future research". Electrochimica Acta 2000, 45, 2499-2513.
2. Localized electronic states in disordered materials and surface states
Figure 7.7. Model of a nanostructured semiconductor film with a transport state at energy Ec and a broad distribution of localized states in the bandgap. The voltage determines the Fermi level of electrons EFn.

## Slide 5: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.3. Schematic energy diagram of the occupancy of a distribution of localized states in the bandgap in an amorphous semiconductor. The shaded region indicates the bandgap states that are occupied with electrons below the Fermi level.

## Slide 6: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.4. (a) Density of states in the band gap of a-Si:H. edge. (b) Free and trapped charge in the band gap for the DOS distribution.

## Slide 7: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.5. Representation of the chemical capacitance of a monoenergetic energy level at E=0, as a function of the temperature as indicated.
3. Chemical capacitance of a single state
Figure 5.1.

## Slide 8: Reproduced with permission from Chidsey, C. E. D.; Murray, R. W. "Redox capacity and direct current electron conductivity in electroactive materials". The Journal of Physical Chemistry 1986, 90, 1479. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.6. (a) Film capacitance, C, and redox capacity (chemical capacitance), r, and (b) film conductance, G, and dc electron conductivity, of a polymer poly[Os(bpy)2(vpy)2](ClO4)x sandwiched between Pt and porous Au electrodes and immersed in 0.1 M Et4NC1O4/CH3CN.

## Slide 9: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.7.
4. Chemical capacitance of a broad DOS
Figure 7.3.

## Slide 10: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.8. (a) Energy diagram showing the thermal occupation at temperature T=300 K of an exponential DOS in the bandgap. EF is the Fermi level of electrons and EC is the conduction band energy. The clear shaded region indicates the bandgap states that are occupied with electrons, and the dark shaded region indicates empty levels, as determined by the Fermi-Dirac distribution function (dashed line). Parameters used in the calculation: T=300 K, T0=800 K , NL=1020 cm-3.

## Slide 11: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.9. (a) Representation of an arbitrary DOS ( , ), the Fermi Dirac function for occupation of electrons and holes, and the product with . (b) Representation of for EF varying at steps of 0.1 eV from 0.1 eV to 0.9 eV.

## Slide 12: © Juan Bisquert Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.10. Energy diagram of a double Gaussian DOS in linear (a) and logarithmic (b) scale of the density of states. The bottom Gaussian has centre E1=-1 eV, total density N1= 10 and dispersion parameter σ1 = 0.1 eV. For the top Gaussian E2 = 1 eV, N2= 30 and E2= 0.2 eV. The filled areas correspond to the occupied states at T = 300 K at the Fermi level positions -1.4, -1.0 and 0.0 eV, from bottom to top.
5. Filling a DOS with carriers: the voltage and the conductivity

## Slide 13: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.11. The charging (chemical capacitance, dashed line) and in situ conductivity measurement (thin line) of thin film terthiophene functionalized polyphenylene core dendrimer at T=300K . Reproduced with permission from John, H.; Bauer, R.; Espindola, P.; Sonar, P.; Heinze, J.; Müllen, K. "3D-Hybrid networks with controllable electrical conductivity from the electrochemical deposition of terthiophene-functionalized polyphenylene dendrimers". Angewandte Chemie International Edition 2005, 44, 2447-2451.

## Slide 14: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
6. Chemical capacitance of Li intercalation materials
Figure 5.23

## Slide 15: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.12. Experimental derivative curves for LixMn2O4. Reproduced with permission from Gao, Y.; Reimers, J. N.; Dahn, J. R. "Changes in the voltage profile of Li/Li1+xMn2-xO4 cells as a function of x". Physical Review B 1996, 54, 3878-3883.
6. Chemical capacitance of Li intercalation materials
Figure 5.25..

## Slide 16: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.13. The top panel shows the calculated derivative curve for LixMn2O4, and the bottom two panels show the occupations of the two sublattices y1 and y2. They are all plotted versus the voltage. The two vertical dashed lines represent the boundaries between ordered and disordered phases.
Figure 7.12.

## Slide 17: Reproduced with permission from Strömme, M. "Cation intercalation in sputter-deposited W oxide films". Physical Review B 1998, 58, 11015-11022. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.14. (a) Electrode potential as a function of the A/W ratio x (A is Li, Na, or K) as obtained under constant current intercalation into crystalline W oxide. The two regions marked out are analyzed in (b), where full lines represent measured chronopotentiometry and squares (composition region) and circles (composition region 2) are data obtained by fitting to the lattice-gas model. The interaction parameter U and the site energy Ɛ are displayed. (c) Derivative of the composition x with respect to working electrode potential .

## Slide 18: Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.15. (a) Diagram showing the geometry of a graphene MOS structure, where a graphene-Y2O3–Ti/Au capacitor lies on a SiO2 /Si substrate. (b) Optical image showing a device and experimental set up for measurements. The graphene channel is in the dashed frame indicated by the black arrow. The channel area covered by top gate electrode is W/L=4.5 mm/7 mm. The separation between source/drain electrodes to the top gate electrode is 12 mm. (c) Total gate capacitance of the as fabricated graphene FET. Inset: gate leakage current density as a function of gate voltage. (d) Quantum capacitance of graphene extracted from (c). The dashed line is the theoretical value of quantum capacitance of graphene at 300 K with a Fermi velocity 1.15x106 m s-1. Reproduced with permission from Xu, H.; Zhang, Z.; Peng, L.-M. "Measurements and microscopic model of quantum capacitance in graphene". Applied Physics Letters 2011, 98, 133122.
7. Chemical capacitance of graphene

## Slide 19: Reproduced with permission from Fang, T.; Konar, A.; Xing, H.; Jena, D. "Carrier statistics and quantum capacitance of graphene sheets and ribbons". Applied Physics Letters 2007, 91, 092109. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.16. Left: quantum capacitance of 2D graphene and a 5 nm GNR compared with the parallel-plate capacitance of 1 nm SiO2 and HfO2. Right: 2D carrier density in a graphene sheet as a function of gate voltage for different oxide thicknesses.

## Slide 20: Reproduced with permission from Xia, J.; Chen, F.; Li, J.; Tao, N. "Measurement of the quantum capacitance of graphene". Nature Nanotechnology 2009, 4, 505-509. Juan Bisquert Nanostructured Energy Devices: Equilibrium Concepts and Kinetics CRC Press
Figure 7.17. (a) Schematic of the quantum capacitance measurement setup in which a graphene sheet on a silicon/SiO2 substrate is connected to a gold electrode. The edge of the graphene sheet is covered with an insulation layer so that only the top surface is exposed to an ionic liquid electrolyte. The potential of the graphene is controlled and varied with respect to a platinum reference electrode (RE) using a three-electrode electrochemical configuration. , electrochemical gate voltage. The inset is an optical micrograph of the graphene device. (b) Total capacitance (blue line) and quantum capacitance (red line) of graphene measured in ionic liquid.